## Slide 1: 2015 Local Roads Workshop Gaylord March 12, 2015

## Slide 2
Best Practices for HMA Construction

## Slide 3
HMA Construction Inspection
Sound inspection practices during construction are vital to obtain quality
Both Agency and Contractor are responsible
Process control and acceptance procedures alone will not ensure quality
Key components of Inspection are:
  Enforcement of specifications
  Ensure good practices are being used
  Observation of materials and workmanship

## Slide 4
HMA Construction Inspection

## Slide 5
What is Quality?

## Slide 6
Definition of Quality for HMA
How do we define Quality?
  Meets Agency mixture specifications
  Meets Agency density specifications
  Smooth riding surface
  Uniform texture and appearance
  Obtains expected service life
  Long Lasting asphalt pavement

## Slide 7
Responsibilities
  Represent the owner’s interests
  Keep daily construction diary
  Monitor ambient air and mat temperatures
  Track tonnage with truck tickets
  Calculate yield
  Monitor compaction with nuclear or non-nuclear gauge
  Observe materials and workmanship
  Make sure that good practices are being used
HMA Construction Inspection

## Slide 8
Usually spelled out in specifications
  Checking yield/thickness of materials being placed
  Adhering to weather and temperature limitations
  Checking mix and mat temperature
  Acceptance testing of final density
Routine Duties of Inspector

## Slide 9
MDOT Temperature and Weather Limitations
  Min temp 35 deg. F, min. 200 lbs/syd
  Min temp 40 deg. F, min. 120 lbs/syd
  Min temp 50 deg. F, any course
Temperature and Weather Limitations

## Slide 10
Min. and Max. Mix Temperatures
Notes: MDOT will reject loads with a mix temperature either below 250 deg. F, or greater than +/- 20 deg. F from the recommended maximum mixing temperature specified by the binder producer at the time of discharge from behind the screed.

## Slide 11
Why does it matter if the mix is too cold?
  Because the mix stiffens as it cools. This makes it difficult to obtain proper roadway compaction.
  Proper roadway compaction is probably THE most important factor in determining the logevity of the roadway. Every effort must be made to obtain the target density during the compaction process.
Temperature and Weather Limitations

## Slide 12
What about maximum mix temperature?
Temperature and Weather Limitations
Notes: MDOT will reject loads with a mix temperature either below 250 deg. F, or greater than +/- 20 deg. F from the recommended maximum mixing temperature specified by the binder producer at the time of discharge from behind the screed.

## Slide 13
Why does it matter if the mix is too hot?
  Because the lighter fractions of the asphalt binder evaporate at higher temperatures.
  This makes the remaining binder stiffer, and causes early aging of the binder. Aged binder tends to be more brittle, and more suseptable to cracking.
Temperature and Weather Limitations

## Slide 14
Measuring Density
Density Acceptance
Using cores . . .
or density gauge

## Slide 15
Watch for Segregation
Truck-end segregation is caused by segregation in the truck transferred to the paver.
Make sure the trucks are being loaded in multiple drops!

## Slide 16
Hauling
  Provide a steady flow of material to the paving operation
  Deliver mix at consistent and correct temperature
  Paving
  Continuous operation (keep paver moving)
  Compaction
  Compact mix when it is hot
Best Practices

## Slide 17
Surface Prep – Good Practice?

## Slide 18
Poor Tack Application

## Slide 19
Tack Coat
To promote the bond between old and new layers.
To prevent slippage between layers
To provide an additional moisture barrier, especially when applied along transverse and longitudinal vertical surfaces
Why do we use Tack Coat?
MS-22
5-10

## Slide 20
Tack Coat
SS-1, but also SS-1h, CSS-1, CSS-1h, CRS-2, or straight binder
Clean before applying
Coat surfaces that will contact new HMA
Watch accidental pick-up
  Tracking
Do not apply:
  In cold or windy weather
  Or on wet surfaces with free water

## Slide 21
Tack Coat
Original emulsion is often diluted at 1:1 ratio
  Ehance sprayability
  Apply at a rate of 0.05 to 0.15 gal/yd2
Adjusted based on surface texture
  Less on smooth
  More on rough)
Make sure tack breaks before paving
Advice: Don’t allow the tack too far in advance of paving
Wind blown dust & debris minimizes its effectiveness

## Slide 22
Tack Coat
GOOD
Even uniform coverage
No puddles
No stripes
BAD
Uneven coverage
Clogged nozzles / improper orientation
Stripes are clearly visible

## Slide 23
Tack Coat
Full width of mat to minimize movement of unsupported edge
Photo Courtesy of Jim Scherocman
Notes: The application of a properly cured tack coat (PG grade or emulsion) is critical to minimizing the lateral movement of the unsupported edge. It is important the tack coat cover the full width of the lane being placed. In the photo above, the tack was placed beyond the edge of the mat, which is OK too.

## Slide 24
HMA Construction Inspection
Sound inspection practices during construction are vital to obtain quality
Both Agency and Contractor are responsible
Process control and acceptance procedures alone will not ensure quality
Key components of Inspection are:
  Enforcement of specifications
  Ensure good practices are being used
  Observation of materials and workmanship

## Slide 25
Questions?
Best Practices for HMA Construction