## Slide 1: 2015 Local Roads Workshop Gaylord March 12, 2015

## Slide 2
Project Scoping

## Slide 3
Decision Making Process
Mix Selection
Rehab of Concrete Pavements
Preventive Maintenance
Presentation Outline

## Slide 4: Decision Making Process
Pavement Management

## Slide 5: Decision Making Process
  Determine current pavement condition
  Predict future pavement condition with and without work
  Determine where, when and what work to do
  Get organized by knowing your pavement inventory
  Justify budget needs
  Determine what works and what doesn’t (e.g., feedback loop)
Purpose of PMS

## Slide 6: Decision Making Process
PMS Process
Pavement
Data
Collection
Project
evaluation
Select
feasible
alternatives
Reconstruction
Rehabilitation
Resurfacing
Life - cycle
costs
Non-
monetary
factors
Select
preferred
alternatives
Detailed
PS & E
Construction
Monitor
Performance

## Slide 7: Decision Making Process
Asset Management Strategy
12% OF
LIFE
EXCELLENT
GOOD
FAIR
POOR
VERY POOR
FAILED
40% DROP
IN QUALITY
40% DROP
IN QUALITY
75% OF LIFE
MAY COST $1.00 FOR
RENOVATION HERE
MAY COST
$4.00 TO $5.00
HERE
TIME

## Slide 8: Decision Making Process
Pavement Inventory
Inspection
Condition Assessment based on inspection results (e.g., PASER rating, PCI, RSL, etc.)
Prediction Modeling technology for developing deterioration trends
Network Condition Analysis
Annual and long Range Work Planning
Components of PMS

## Slide 9: Decision Making Process
Type of Data to be Collected
  Physical characteristics
  Construction and maintenance history
  Traffic levels
  Climate information
  Soils information
Network Inventory

## Slide 10: Decision Making Process
The assessment of current condition MUST be objective and repeatable
BUT, it must also match available resources
All system recommendations are based on the current and predicted conditions of the sections in your network
Condition Assessment

## Slide 11: Approaches to Collecting Pavement Condition Data
Manual
Semi-automated
Automated
Decision Making Process

## Slide 12: Decision Making Process
Rating Scale 1 - 10
  Rating of 1 represents a condition needing total replacement.
  Rating of 10 represents the best, or new construction.
Surface Condition
  Important to public
  Simplified PMS system
PASER – Pavement Surface Evaluation and Rating System

## Slide 13
Decision Making Process
Mix Selection
Rehab of Concrete Pavements
Preventive Maintenance
Presentation Outline

## Slide 14
Mix Selection – Mix of Fixes
Capital Preventive Maintenance - (Crack Filling, Surface treatments, thin overlays)
Rehabilitation - Conventional overlays, Rubblization, ASCRL, Etc.
Reconstruction - Full depth pavement removal and replacement (10 – 13 inches)
Notes: We support the concept of using a “mix of fixes” approach to pavement management:
Preventive maintenance - (Crack Filling, Surface treatments, thin overlays)
Rehabilitation - Conventional overlays (3 to 6.5 inches, usually with base preparation)
Reconstruction - Full depth pavement removal and replacement (10 – 13 inches)
This Provides a system for pavement owners to select an optimal combination of fixes to achieve system condition goals at the lowest total cost.
It is important to acknowledge that pavements do eventually wear out. We are going to have to reconstruct and rehabilitate some of the roads – we can’t just rely on preventive maintenance to achieve sustainable pavement conditions.

## Slide 15
Mix of Fixes
Capital Preventive maintenance: Shorter Term Fixes
  1 ½” HMA Overlay
  Milling and 1 ½” HMA Overlay
  Crack Treatment
  Overband Crack Filling
  Chip Seal
  Micro-Surfacing
  Ultra-Thin HMA Overlay

## Slide 16
Mix of Fixes
Rehabilitation: Medium Term Fixes
  Structural HMA Overlay (Multiple Course)
  Mill and Structural HMA Overlay
  In-Place Recycling
    Crush and Shape
    Cold-in-Place
    Hot-in-Place
    Full Depth Reclamation
  Rubblization
  ASCRL

## Slide 17
Mix of Fixes
Reconstruction: Long Term Fixes
  Full depth pavement removal and replacement (10 – 13 inches)
  New Construction

## Slide 18: Selecting the Right Mix
Selection of Mix for:
  Optimum Performance
  Economics
Binder Selection Economics
Lift Thickness vs. Performance
Use of RAP
Notes: Minimum lift thickness is not always good!

## Slide 19: Binder Selection
Example:
1 ½” resurfacing of existing road
  98% reliability binder grade is PG 64-28
Consider using PG 64-22 ?
  Reflective cracking
Notes: Good example - especially if a shorter term fix ( 7-9 yrs)
Or 58-34, consider using 58-28

## Slide 20: Lift Thickness based on Nominal Maximum Aggregate Size (NMAS)
NMAS – 1 size larger than the first sieve to retain more than 10%

## Slide 21: NMAS
Ex: 4C mix – NMAS is ½”
Notes: Example, 4C mix – NMAS is ½ inch

## Slide 22: Local Agency Programs HMA Selection Guidelines
Mixture Type | Marshall Mixture |  |  |  |  | Superpave Mixture |  | 
 | 36A | 13A | 2C | 3C | 4C | 3E_ | 4E_ | 5E_
Min. #/syd | 110 | 165 | 350 | 220 | 165 | 330 | 220 | 165
Max. #/syd | 165 | 275 | 500 | 330 | 275 | 410 | 275 | 220
Note: Application Rate of 110#/syd. Per 1 inch Thickness
Notes: HMA Mixture Type Application Rates
Lift thicknesses based on NMAS (nominal Max Aggregate size)
For Marshall mixes: Min LT, generally 3X NMAS, Max LT, generally 5X NMAS
For Superpave mixes: Min LT, 4X NMAS, Max LT, 5X NMAS

## Slide 23: Lift Thickness vs. Performance
In-place Density is Critical
  Initial In-place Air Voids <8%
Lift Thickness Affects Compaction
  Consolidation “Room”
  Cooling Rate
Notes: Place mixes at least at the minimum lift thickness recommended
  Initial In-place Air Voids <8% non permeable
Consolidation “Room” - aggregate particles have squeeze all together
  Cooling Rate - thin lifts cool quicker

## Slide 24: Why Recycle RAP into HMA?
Best and Highest use
Same or better performance as virgin mix
Reduces demand for new materials
Reduces carbon footprint
Contains valuable materials
Save $
Notes: It is estimated that recycling of asphalt pavements saves the American taxpayer $1.8 billion per year. It also saves hundreds of acres of landfill space each year.
Reclaimed asphalt pavement (RAP) can be recycled into pavement that is as high, or even higher, in quality as pavements made of all-virgin materials. And, the same material can be recycled again and again; it never loses its value. The asphalt cement—the glue that holds the pavement
together—retains its ability to function as glue or cement, so that it is reused for its original purpose. The aggregates in the original pavement
are also conserved.
HMA pavements are 100% recyclable, when you invest in HMA pavements, by using RAP you can get a return on your original investment by re-using the liquid AC and aggregates. In contrast, when using PCC, the cement represents a cost, it can not be re-used.
Taking advantage of these valuable materials can help stretch your pavement budget and get roads improved .
24

## Slide 25: Why Recycle RAP into HMA?
RAP contains valuable materials :
  Aggregate ~ 94% @ $10/ton
  Asphalt ~ 6% @ $585/ton
  Value = $44.50 /ton (minus processing)
Notes: The $ 44 / ton in place value of the materials is probably more than the original price of the mix laid in place !
Like $ in the bank . ( return on investment )
25

## Slide 26: Economics Savings Example
Material | 0% RAP | 17% RAP | 27% RAP
Aggregate | $9.40 | $7.70 | $6.70
Asphalt | $35.10 | $29.13 | $25.62
RAP |  | $1.53 | $2.43
Total | $44.50 | $38.36 | $34.75
$ Savings |  | $6.14 | $9.75
% Savings |  | 13.8% | 21.9%
Aggregate: $10.00/ton
Asphalt: $585.00/ton
RAP: $9.00
Mix Design AC Content: 6.0%
Notes: One last example
??????

## Slide 27
Follow best practices for the processing and management of RAP
Contractor to sample and test RAP during processing
RAP usage specification
RAP mixes should meet same specs as virgin mixes
Adjust binder grade appropriately
Approved mix design including RAP
Recommended Practices for Use of RAP (and RAS)
Notes: MDOT Requirements :
Perform specified quality control testing of the RAP during the
processing and stockpiling of the RAP..
Perform a complete mixture analysis, including gradation
of aggregate, asphalt binder content and theoretical maximum
specific gravity, for every 1000 tons of processed RAP. ( MDOT form 1879 )
IF RAP stockpile is less than 3000 tons , need a min of 3 complete tests ( with GMM and Gse )
(Note Gse is calculated from GMM and Ac content )

## Slide 28
Approved mix design including RAP
Know the properties of the RAP
Gradation , binder content ,
theoretical maximum specific gravity
Mix design must be done incorporating RAP and taking into account the RAP characteristics
Recommended Practices for Use of RAP
Notes: MDOT Requirements :
Perform specified quality control testing of the RAP during the
processing and stockpiling of the RAP..
Perform a complete mixture analysis, including gradation
of aggregate, asphalt binder content and theoretical maximum
specific gravity, for every 1000 tons of processed RAP.

## Slide 29
Mix Design Example
Notes: Mix design must be done incorporating RAP and taking into account the RAP characteristics
15 % RAP mix ( Rap has 3.6 % AC )
Add - 5.16 % new AC - to get 5 .7 % final design AC

## Slide 30: Ability to Meet Volumetrics
Treat RAP as mix component
Challenges: VMA and dust/asphalt ratio
  Good processing practices and quality control can be used to overcome this issue
Notes: RAP has a higher dust content than the other aggregates used in todays asphalt mixes
Has to be managed and controlled just like any other component in the mix in order to meet mix volumetric properties
  Good processing practices can be used to overcome this issue
    Minimize generating dust in RAP stockpiles
    Fractionate RAP for mix design flexibility and gradation control

## Slide 31
Test the produced Mix:
(Binder, Gradation)
Contractor Quality Control Tests
Owner Quality Assurance / Acceptance tests
If you have performance concerns:
Consider testing/monitoring other properties
Mix volumetrics (Air Voids, VMA)
Fines to Effective Binder Ratio
Recommended Practices for Use of RAP (and RAS)

## Slide 32
Decision Making Process
Mix Selection
Rehab of Concrete Pavements
Preventive Maintenance
Presentation Outline

## Slide 33: Rehabilitation of Concrete Pavements
Improve ride quality
Correct surface defects
  improve surface drainage
  increase surface friction
Delay/prevent structural deterioration
Strengthen pavement structure (rehabilitation)
Notes: Concrete rubblization followed by an HMA overlay improves ride quality by removing bumps caused by faulting in joints and cracks.
It corrects surface defects in the roadway providing improved surface drainage. The elimination of joints and faults keeps water from ponding as readily. Surface friction is improved by reducing hydroplaning potential.
Deterioration of the structure is slowed by preventing the intrusion of surface water into the old concrete. This is especially important when durability cracking is present in the old PCC. By eliminating the water, the action of freeze-thaw cycles is greatly diminished.
Because a substantial structural overlay is placed on the rubblized concrete, the pavement is strengthened for future traffic.

## Slide 34: Rehabilitation Design Factors
Condition of existing pavement
  Drainage
  Distress
  Response to load
Foundation strength/stiffness
  Subbase
  Subgrade
Future traffic loading
Additional corrections (safety, capacity, etc)
Notes: As with any pavement design, rubblization requires good site investigation, planning and design in order to be successful.
The type of concrete pavement and its thickness will dictate the effort necessary to fracture the slab. For instance, a thin, plain jointed concrete pavement will require less fracture energy than a thick continuously reinforced concrete pavement.
The adequacy of drainage, types of surface distress and structural integrity of the existing pavement need to be considered in the rubblization and overlay thickness design.
The subgrade type and its stiffness and strength are important considerations. If the PCC slabs are lying directly on a fine-grained soil that is close to saturation, the rubblization process may cause the material to liquify. It is important to carry out a good site investigation to identify possible problems.
The HMA overlay thickness must be such that future traffic demands are met.
Attention must be also be given to other project aspects such as correcting alignments or adding capacity. It is important that details such as maintaining drainage flow are considered in the planning and design stages.

## Slide 35: Reflective Cracking
PCC
By far, the biggest problem in HMA overlays of PCC pavement
Caused by movement at PCC joints and cracks
Load-induced movement
Joint Closes
HMA
Slabs Contract
Joint Opens
Slabs Expand
Reflective crack
Notes: The most common form of distress in HMA overlays of PCC is reflective cracking. This is a result of the concrete slabs contracting and expanding with temperature changes, which cause the joints and cracks to open and close. This opening and closing causes a crack to form in the HMA directly over the opening in the concrete.
Also, if the concrete slabs are not firmly seated on the underlying material, traffic loads going over the joints will cause the joints to move up and down vertically. This movement will cause shearing in the asphalt over the joint and create a reflective crack.

## Slide 36: Design Issues
Rate of propagation through overlay
Number of reflected cracks
Rate of deterioration of reflected cracks
Amount of water that can infiltrate through the cracks

## Slide 37: Reflection Crack Control Measures
Fabrics
Stress-relieving interlayers
Crack-arresting interlayers
Preoverlay treatments
Slab repair or replacement
Sawing and sealing joints
Increased overlay thickness

## Slide 38: Crack Control Effectiveness
Delay the occurrence of cracking
Reduce the number of cracks
Control the crack severity
Provide other benefits
  Reduce overlay thickness
  Enhance waterproofing capabilities

## Slide 39: Fabrics
Old pavement
Vertical differential
Movement
Stress concentration
Overlay
Subgrade Soil
Horizontal opening
Fabric

## Slide 40: Fabric Application

## Slide 41: Pre-overlay Repairs
Slab stabilization
Fractured slabs
Slab repair / replacement
Load transfer restoration

## Slide 42: Fractured Slab Techniques
Crack and seat (JPCP)
Break and seat (JRCP)
Rubblize (JPCP, JRCP, CRCP)

## Slide 43: Cracking and Seating
Shortens effective slab length
Standard practice in many States
Not “generally” recommended for use on poor subgrades
Design methods (overlay thickness)

## Slide 44: Cracking and Seating
Overlay
Subgrade Soil
Subbase
Firm Foundation
Cracks
Short slab length (~2’)
Good
granular
interlock

## Slide 45: Cracking and Seating

## Slide 46: Cracking and Seating

## Slide 47: Rubblization
Fracturing:
  Eliminates slab action
  Destroys bond between concrete and steel
Rubblized base responds as a tightly keyed, interlocked high-density, unbound layer
  Layer cannot crack; already fractured
Notes: Rubblization eliminates slab action by 1) destroying the geometry of the slab and 2) seating the concrete firmly against the underlying subbase or soil. It also breaks the bond between the concrete and any steel present in the slab, eliminating detrimental effects caused by corrosion of the steel and further reducing the ability of the concrete to act as a mass.
The rubblized concrete responds as a tightly packed, high-density granular material. The rough, hard particles provide an internal friction to resist rutting while the lack of tension prevents cracking.

## Slide 48: Why Rubblize?
Fracturing PCC to segments less than 9” precludes reflection of:
  Joints
  Cracks
  Faults
Production Rates up to 1 lane-mile/day
Notes: Fracturing the surface of the concrete to a relatively small size means that features and problems in the old concrete surface such as joints, cracks and faults cannot reappear in the HMA overlay. This prolongs the life of the overlay and helps to ensure a smooth pavement.
Production rates with rubblization are up to 1 lane-mile per day, per rubblizer, much faster than other types of PCC rehabilitation. This means lower construction costs and less inconvenience to road users, giving substance to the slogan “Get In, Get Out, Stay Out.”

## Slide 49
HMA
PCC
Smaller Pieces = Smaller Movement = No Cracking
Rubblization
Notes: Rubblization reduces the size of concrete pieces so that the expansion and contraction causes a minimum of movement. The space between the fractured pieces moves less so that the cracks are not reflected through the surface. And, because the process seats the pieces of concrete, reflection cracking through shearing at the joints does not occur.

## Slide 50: Rubblization - Equipment
Notes: The Resonant Pavement Breaker (RPB) uses a low-amplitude 2000-pound force applied at a frequency of 44 cycles per second to fracture the concrete pavement.

## Slide 51: When to Rubblize
    Patching > 10%.
    Severe D-cracking.
    Severe ASR or ACR cracking.
    Dowel bar locking
    Severe joint deterioration
    Persistent faulting.
Notes: Some general guidelines on when to rubblize concrete pavement include:
When patching is needed in more than 10% of the slab,
When severe durability (D) cracking is present,
Alkali-silica reaction (ASR) or alkali-carbonate reaction (ACR) cracking is present,
When dowel bars have locked up due to corrosion,
When faulting reappears shortly after retexturing the concrete surface.
All these distresses are indications that major systemic problems exist in the concrete pavement, and that a rehabilitation consisting of rubblization with an HMA overlay is viable.

## Slide 52
Weak soils may make construction difficult.
Option 1
  Adjust breaking pattern (12 - 18”) in soft areas.
  Use normal seating rolling.
  Resume smaller pattern after weak area.
Precaution
Notes: It is not unusual to run into occasional soft spots of soil. In these conditions, rubblization may weaken the soils and cause the rubblized particles to punch through the underlying material. When this happens, there are a couple of options which should be immediately considered.
The first option is to reduce the effort in fracturing the slab. This can be done by adjusting the breaking pattern to produce larger pieces. If the softening seems to stop, then use a normal rolling pattern to seat the concrete and resume the original pattern after the soft area.

## Slide 53
Option 2
  Cease rubblization
  Define weak area
  Remove/replace problem material
  Resume normal operations when past weak area
Perform a good soils evaluation prior to construction
Precaution
Notes: The next option is to cease rubblization. This should be done if adjusting the breaking pattern does not work. The area of soft soil should be defined to mark the limits. The concrete should be removed along with the problem soil in the local area. Normal rubblization operations can proceed after the soft area.
These types of problems may be reduced significantly if a good soils investigation is performed ahead of construction. Past project records, soils maps and non-destructive testing may provide vital clues to identifying problem areas.

## Slide 54: Stress-Absorbing Interlayers
Old pavement
Vertical differential
Movement
Stress concentration
Membrane
Subgrade Soil
Horizontal opening
Overlay

## Slide 55: Asphalt Stabilized Crack-Relief Layer (ASCRL)
Old pavement
HMA Overlay
Subgrade
ASCRL High voids
Notes: Grade lift or ASCRL

## Slide 56: Asphalt Stabilized Crack-Relief Layer (ASCRL)

## Slide 57: Asphalt Stabilized Crack-Relief Layer (ASCRL)
Old pavement
HMA Overlay, 3.5” – 4”
Subgrade
ASCRL 3” – 3.5”
Notes: Grade lift or ASCRL

## Slide 58: Asphalt Stabilized Crack-Relief Layer (ASCRL)
Notes: MDOT has a special provision

## Slide 59: Asphalt Stabilized Crack-Relief Layer (ASCRL)

## Slide 60: Asphalt Stabilized Crack-Relief Layer (ASCRL)

## Slide 61: Asphalt Stabilized Crack-Relief Layer (ASCRL)
Mix Design
  Asphalt Binder – PG 64-28 with 0.5% liquid antistrip additive
  Asphalt content – 3 to 4 %
  Surface Coating – 100 % without excessive draindown (max 0.30 %)
  Minimum Asphalt film thickness - 9.0 microns
  Moisture sensitivity (AASHTO T283)

## Slide 62: Asphalt Stabilized Crack-Relief Layer (ASCRL)
Construction
  Placed in a single layer
  Compaction – steel – wheeled tandem roller (1.0 ton per foot of drum length)
    Static mode only
    Minimum of three passes (down and back)
    Compaction test strip may be required (minimize breakage of Agg.)

## Slide 63: Asphalt Stabilized Crack-Relief Layer (ASCRL)
Project | # of Jobs | Length (miles)
ASCRL | 25 | 105
MDOT Projects to Date
Started in 2001
  All are performing very well

## Slide 64: Asphalt Stabilized Crack-Relief Layer (ASCRL)
M-21, Before Construction
Notes: This section of M-21 was going to be done in 2012, date of pic

## Slide 65: Asphalt Stabilized Crack-Relief Layer (ASCRL)
M-21, 3 years old
Notes: This section of M-21 was done in 2009, pic is from 2012, just down the road from previous slide pic

## Slide 66: Sawing and Sealing Joints
Concede appearance of reflection cracking
Objective: control rate of deterioration
Reduces spalling of reflection cracks
Candidates should have well-defined joints
Sawcut must be directly above underlying joint

## Slide 67: Sawing and Sealing Joints
Reflection crack
Overlay
Old pavement
Sealant
Initial sawcut
1/3 depth
Horizontal opening
Joint reservoir
Subgrade
Vertical differential movement

## Slide 68: Sawing and Sealing Joints

## Slide 69: Increased Overlay Thickness
Delays occurrence of reflection cracking
Cracks propagate about 1 in. per year
Reduces temperature fluctuations in underlying pavement

## Slide 70
Decision Making Process
Mix Selection
Rehab of Concrete Pavements
Preventive Maintenance
Presentation Outline

## Slide 71
Preventive Maintenance

## Slide 72
Preventive maintenance is a planned strategy of cost effective treatments to an existing roadway system and its appurtenances that preserves the system, retards future deterioration, and maintains or improves the functional condition of the system without substantially increasing structural capacity.
Preventive Maintenance
Notes: The Capital Preventive Maintenance (CPM) Program was established to preserve the structural integrity and extend the service life of the state trunkline network through a series of construction contracts. The program was initiated by the Michigan Department of Transportation's Maintenance Division (currently the program resides in the Construction and Technology Division) in 1992, in cooperation with the Federal Highway Administration. Funding for the program is a combination of federal and state transportation dollars.

## Slide 73
Standard Capital Preventive Maintenance Treatment
Pavement Seal
HMA Crack Treatment
Overband Crack Fill- Pretreatment
Chip Seals
Micro-surfacing
Ultra-Thin HMA Overlay-Low & Medium Volume (<1″ thick)
Shoulder Fog Seal
Paver Placed Surface Seal
Preventive Maintenance
Notes: The CPM program has two subgroups, Pavement Sealing and Functional Enhancements, to encourage a balanced CPM strategy that will complement the Regions Road Rehabilitation/Reconstruction strategy. A discretionary budget and an emerging technologies budget also exist to supplement either group to achieve the most cost effective preventive maintenance strategy. The discretionary budget can be used for pavement sealing, functional enhancements, or emerging technologies. Emerging technologies are new treatments that are promising, but whose performance and cost effectiveness are unknown.

## Slide 74
Crack Treatment
Preventive Maintenance

## Slide 75
Chip Seal
Preventive Maintenance

## Slide 76
Micro-surfacing
Preventive Maintenance

## Slide 77
Extends pavement life Protects pavement structure Restores pavement smoothness
High Value Pavement Enhancement
HMA Ultra-Thin
Preventive Maintenance
Notes: HMA Ultra-Thin is the High value pavement enhancement.
It will extend the life of your pavement,
Protect the pavement structure,
And restore pavement smoothness.

## Slide 78
HMA Ultra-Thin
BENEFITS
• 5-9 year life extension
• Seals pavement to delay further deterioration
• Improve ride quality
• Minimize or eliminate structure adjustments
• Reduce noise
• Improve drainage
• Ease of construction, standard paving operation
• Minimal construction time
Notes: BENEFITS
• 5-9 year life extension
• Seals pavement to delay further deterioration
• Improve ride quality
• Can improve skid resistance
• Maintain existing gutter pan
• Minimize or eliminate structure adjustments
• Reduce noise
• Improve drainage
• Ease of construction, standard paving operation
• Minimal construction time

## Slide 79
Treatment | $/syd | Cost/mile (24’ wide) | MDOT Life extension range (years)* | MDOT Life extension range average (years)* | Cost/mile* per year
Double chip seal | $3.13 | $44,069 | 3-5 | 4 | $11,017
Micro-surface | $3.02 | $42,520 | 3-5 | 4 | $10,630
Ultra-thin low | $3.09 | $43,505 | 5-9 | 7* | $6,215
Ultra-thin med | $2.83 | $39,845 | 5-9 | 7* | $5,692
Ultra-thin high | $3.29 | $46,321 | 5-9 | 7* | $6,617
Preventive Maintenance Treatment Cost Comparison
*Average Life Extension estimated by APAM
Unit Prices based on MDOT Information (thru Jan. 2015)
HMA Ultra-Thin
Notes: HMA Ultra-Thin is Your Best Value for Preventive Maintenance dollars!
As You can see, the cost/mile per year is much lower than that of chip seal or microsurfacing.

## Slide 80
HMA UT Chip Seal Microsurfacing
HMA Ultra-Thin

## Slide 81
Advantages:
Adds structural value
Very smooth riding surface
Improved ride quality
No excess stone buildup
No broken windshields from loose aggregate
HMA Ultra-Thin

## Slide 82
Questions?
Project Scoping